SECTION 09 97 23

LIME-BASED SAND FINISH PLASTER

(TONACHINO FIRENZE® – EXTERIOR)

Mature Lime Putty Decorative Finish – Fine Grain Matte Texture

Notes to Specifier: Information shown in boxes is for specifier use only and should not be included in the final project specifications. Meoded is the premier US manufacturer of natural mineral-based paints and lime plasters. Some products are intended for interior use only, while others are formulated for exterior applications, offering resistance to weather, UV exposure, and color stability. With a wide variety of colors and textures, Meoded systems offer versatile design possibilities, featuring a range of sheen levels, visual depth, movement, and natural stone textures. The specifier shall select the appropriate product from the Meoded line in accordance with the required color, texture, sheen, and finish to achieve the desired result. Modify this specification as needed to suit the project substrates. For assistance with product selection, color samples, or review of project specifications, contact Meoded at (323) 308-2600. Meoded is a manufacturer only and does not perform installation. Responsibility is limited to the manufacture of its decorative finishes and does not extend to defects arising from installation methods, substrate conditions, or other non-manufacturing factors. The following is provided as a general guide for specifying applications of Meoded Tonachino Firenze® and does not constitute approval of materials or methods not supplied or expressly recommended by Meoded. Installation methods may vary based on field conditions and applicator technique. Application results are dependent upon substrate conditions, environmental factors, and applicator skill, all of which are beyond the manufacturer’s control. Coordinate related sections to ensure proper substrate preparation. Due to the thin application of Tonachino Firenze®, surface irregularities may be visible. Careful consideration should be given when specifying substrates to clearly define acceptable quality levels. Exterior Substrates: Provide cement plaster (stucco) systems in accordance with ASTM C926, including lath, scratch coat, and brown coat assemblies. Brown coat shall be properly cured (minimum 7 days, 21 days recommended) prior to application of finish. For enhanced crack resistance and substrate stability, application of a reinforced base coat (cementitious base such as CI base, Polybond, or equivalent) with embedded alkali-resistant mesh is recommended prior to primer application. Tonachino Firenze® may be applied over properly prepared exterior substrates including: - Portland cement plaster (stucco) - Concrete and masonry - Cementitious base coats with mesh reinforcement Plaster: Tonachino Firenze® shall be applied over properly prepared exterior cementitious substrates, including two- and three-coat Portland cement plaster (stucco) systems in accordance with ASTM C926. Substrates shall be finished to a true, flat surface suitable to receive thin decorative finishes. Include and honor all expansion joints, control joints, corner beads, flashings, and trim components as part of the system. Do not bridge joints. Tonachino Firenze® may also be applied over properly prepared, stable, and compatible exterior substrates as recommended by the manufacturer. Consult manufacturer for project-specific substrate preparation recommendations. Final appearance is dependent on substrate quality, application technique, and field conditions. Variations in finish are inherent to hand-applied decorative plaster systems and should be expected. Substrate assembly, including weather-resistive barriers, flashing, and drainage systems, shall be provided by others and is not part of this section. Exterior applications require properly designed and constructed substrate assemblies, including water management detailing and protection from environmental exposure during installation and curing.

PART 1 - GENERAL

1.1 SUMMARY

A. Section Includes: Limestone-based, natural mineral decorative plaster exterior finish.

B. Related Sections:

1. Section 09 24 00 – Portland Cement Plastering

2. Section 07 27 00 – Air Barriers 
3. Section 07 25 00 – Weather Barriers

4. Additional sections covering substrate materials as applicable to the project

1.2 REFERENCES

A. ASTM E84 – Standard Test Method for Surface Burning Characteristics of Building Materials
B. ASTM D1308 – Standard Test Method for Effect of Household Chemicals on Clear and Pigmented Organic Finishes
C. ASTM D2486 – Standard Test Method for Scrub Resistance of Wall Coatings
D. ASTM D3363 – Standard Test Method for Film Hardness by Pencil Test
E. ISO 9001 – Quality Management Systems

F. ASTM C926 – Application of Portland Cement-Based Plaster

G. ASTM C1063 – Installation of Lathing and Furring to Receive Portland Cement-Based Plaster

Referenced standards are provided to establish general performance criteria and evaluation methods applicable to similar coating and plaster systems.

1.3 SUBMITTALS

A. Product Data: Submit current manufacturer’s technical data sheets for all specified materials, including installation procedures and performance characteristics.

B. Shop Drawings: Provide drawings indicating layout, finish locations, color selections, and interface with adjacent construction.

C. Samples: Submit [two] [_______] sets of representative samples, [minimum 5 x 5 inches]  [_________], demonstrating the full range of selected colors and textures. Samples are intended to illustrate general appearance only. Final installed finish will vary based on application technique, environmental conditions, and individual applicator methods. Samples are not intended to represent exact final appearance.

D. Application Guidelines: Submit manufacturer’s complete application instructions, including surface preparation requirements, installation methods, and curing/protection recommendations.

E. Installer Qualifications: Installer shall be experienced in the application of decorative plaster finishes and familiar with manufacturer’s application guidelines.

F. Project Experience: Submit a list of at least five comparable completed projects of similar scope and size, with a minimum of three years of service history. Include project names, locations, and contact information.

G. Maintenance Information: Provide manufacturer’s recommendations for cleaning and maintenance in accordance with Section 01 74 00. Include suggested products, procedures, and maintenance schedules.

1.4 QUALITY ASSURANCE

A. Manufacturer Qualifications: Provide materials manufactured by a company with a minimum of ten (10) years’ experience in the production of decorative plaster and specialty coating systems. Manufacturer shall maintain consistent quality control procedures.

B. Installer Qualifications: Installer shall be experienced in the application of decorative plaster systems or similar specialty finishes and capable of producing work of comparable scope and complexity. Provide documentation of relevant project experience upon request.

C. Technical Support: Manufacturer shall make technical guidance available upon request to assist with product application and installation procedures.

D. Mock-Up:

- Prior to commencement of work, prepare a sample area of each specified finish, approximately [4 feet by 4 feet] [________], at a location designated by the [Architect/Designer]  [_________].

- Mock-up shall demonstrate the intended range of color, texture, and workmanship.

- Approved mock-up shall serve as the standard for the completed work and shall remain in place until project completion. Approved mock-up may be incorporated into the finished work where acceptable. Mock-up establishes the acceptable range of finish characteristics and is not intended to represent an exact uniform finish.

- Mock-up shall demonstrate performance under anticipated exterior lighting and environmental conditions.

E. Material Consistency: Provide materials supplied by a single manufacturer to ensure consistency in appearance and performance. Use products as recommended by the manufacturer for the specified application.

F. Pre-Installation Conference: Conduct a meeting prior to installation to review substrate conditions, surface preparation requirements, application procedures, and coordination with related trades. Attendees shall include the Contractor, applicator, and other relevant parties. Document and distribute meeting outcomes to all participants.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Delivery and Storage: Deliver materials in original, unopened containers with manufacturer’s labels intact. Protect materials during transport and storage from excessive heat, freezing, and direct sunlight. Store in a cool, dry, and well-ventilated area within a temperature range of 45°F to 95°F.

1.6 WARRANTY

A. Manufacturer’s Limited Warranty: Provide manufacturer’s standard limited warranty for a period of five (5) years from date of installation, covering defects in materials when products are used and applied in accordance with manufacturer’s written instructions.

Warranty is subject to the following conditions:

- Products must be applied within ten (10) months of the date of manufacture.

- Substrates shall be properly constructed and prepared in accordance with industry standards and manufacturer’s recommendations.

- Manufacturer reserves the right to inspect the installation prior to resolution of any warranty claim.

Warranty limitations:
This warranty is limited to replacement of defective material or refund of the original purchase price, at the manufacturer’s discretion, upon verification of a valid claim.

This warranty does not cover:

- Improper substrate preparation

- Installation or workmanship errors

- Cracking, movement, or structural conditions

- Aesthetic variations or natural color changes including variations resulting from hand application techniques and environmental conditions.

- Water intrusion or moisture-related issues

- Labor or costs associated with removal or reinstallation

- Damage caused by misuse, neglect, or acts of nature

This warranty is exclusive and in lieu of all other warranties, whether express or implied. Manufacturer shall not be liable for incidental or consequential damages.

1.7 ENVIRONMENTAL CONDITIONS

- Do not apply materials during rain, fog, or when precipitation is expected within 24–48 hours.

- Do not apply in direct sunlight, high winds, or when rapid drying conditions may affect finish quality.

- Application shall be performed when ambient and surface temperatures are between 45°F and 95°F and shall remain within this range during curing.

1.8 SYSTEM LIMITATIONS

- This finish is not intended to serve as a primary waterproofing system.

- Waterproofing, flashing, and drainage shall be provided by others.

- Finish system does not bridge cracks or prevent substrate movement; substrate design, crack control, and structural performance are the responsibility of others.

PART 2 - PRODUCTS

2.1 APPROVED MANUFACTURER:

Meoded Paints & Decoration, Inc.

6314 Santa Monica Blvd, Los Angeles, CA 90038

P: 323-308-2600

E: info@meodedpaint.com

www.meodedPaint.com

2.2 SYSTEM PERFORMANCE REQUIREMENTS

A. Material Composition: Lime-based decorative coating composed of lime, mineral aggregates, and fine sand additives formulated to achieve a breathable, natural textured sand finish. Product shall contain no added volatile organic compounds (VOCs) and comply with applicable regulatory requirements.

B. Surface Burning Characteristics: Provide materials with fire performance characteristics consistent with mineral-based decorative plaster coatings when evaluated in accordance with ASTM E84.

C. Surface Hardness: Provide coating with high surface hardness typical of mineral-based plaster finishes when evaluated in accordance with ASTM D3363.

D. Scrub Resistance: When evaluated in accordance with ASTM D2486, coating shall demonstrate resistance to abrasion under laboratory conditions.

E. Chemical Resistance: Provide coating with limited resistance to common household chemicals consistent with mineral-based decorative finishes when evaluated in accordance with ASTM D1308. Minor visual changes, including discoloration, may occur upon exposure to certain chemicals; such changes are inherent to mineral-based finishes and shall not be considered a defect.

F. Weathering Resistance: Color variation, patina development, and weathering due to UV exposure and environmental conditions are natural characteristics of lime-based finishes and shall not be considered a defect.

G. Vapor Permeability: Lime-based finish shall remain breathable, allowing vapor transmission; moisture-related discoloration, efflorescence, or variation may occur and is inherent to the system.

2.3 FINISHES

A. Product: Meoded Tonachino Firenze® decorative lime-based sand finish plaster coating system.

B. Finish: Finish type and texture shall be as selected by the Architect/Designer from the manufacturer's standard range, including fine grain sand textures.

C. Selection:

- Colors shall be selected from the manufacturer's standard palette (MC-701 through MC-899).

- Custom colors available upon request.

- Custom color matching may result in slight variation from submitted samples.

D. Aesthetic Variation: Final appearance shall exhibit natural variation in tone, texture, and movement inherent to hand-applied lime-based finishes. Such variation is an inherent characteristic of the material and system.

2.4 ACCESSORIES

A. Primer: Provide Meoded Quartz Primer or approved compatible primer suitable for substrate and recommended by manufacturer.

B. Protective Finish:
Provide Meoded Stain Shield sealer as recommended by manufacturer.

PART 3 - EXECUTION

3.1 EXAMINATION

A. Verify substrates are suitable for application.
B. Do not proceed until unsatisfactory conditions have been corrected.

  - PREPARATION

A. Protect adjacent surfaces not scheduled to receive finish.

B. Substrate Preparation:

1. Exterior Cementitious Substrates:

a. Provide lath, scratch coat, and brown coat stucco system in accordance with ASTM C926. 
b. Brown coat shall be true, flat, and free of irregularities and properly cured prior to finish application. 
c. Moist cure brown coat as required to minimize shrinkage cracking.

2. Reinforced Base Preparation (Recommended):

a. Apply cementitious base coat (CI base, Polybond, or approved equivalent) over brown coat. 
b. Embed alkali-resistant fiberglass mesh to improve crack resistance and substrate stability.

3. Priming:

a. Apply Meoded Quartz Primer diluted with up to 25% clean water over prepared substrate. 
b. Allow primer to dry in accordance with manufacturer’s recommendations prior to application of finish.

4.  General Requirements:

a. All substrates shall be clean, dry, and free of dust, dirt, oil, grease, efflorescence, and other contaminants that may affect adhesion or appearance.

b. Substrate shall be suitable to achieve the aesthetic intent of the finish as approved in mock-up and consistent with manufacturer’s recommendations.

c. Priming: Apply Meoded Quartz Primer in accordance with manufacturer’s written instructions.

d. Substrates shall be structurally sound, properly cured, and designed to accommodate movement, drainage, and environmental exposure.

e. Do not apply over substrates exhibiting active cracking, movement, or moisture intrusion without proper remediation.

f. Verify proper installation of weather-resistive barrier and flashing systems prior to application.

3.3 APPLICATION TOOLS

A. Use stainless steel trowels, plastic trowels, spatulas, and other tools recommended by the manufacturer.

B. Tools and techniques shall be consistent with those used to produce approved mock-up.

C.  For light-colored finishes, use manufacturer-recommended specialty trowels, including Meoded Whiteout Trowel or Plastic Trowel, to minimize burnishing marks and prevent discoloration.

3.4 APPLICATION

A. Apply materials in accordance with manufacturer’s written instructions.

B. Apply in multiple thin coats to achieve specified texture and appearance.

C. Maintain consistent technique to match approved mock-up. Variations resulting from individual applicator technique are inherent to the system.

D. Do not bridge expansion joints, control joints, or substrate transitions.

E. Apply only when ambient and surface temperatures are between 45°F and 95°F, or within manufacturer’s recommended range.

F. Materials shall be thoroughly mixed prior to application to ensure uniform consistency. Do not over-dilute or alter material beyond manufacturer’s recommendations.

G. Protect applied material from rain, wind, freezing, and rapid drying during application and curing.

H. Do not apply over saturated substrates or when substrate moisture content is excessive.

I. Protect surrounding construction and adjacent materials from staining during application.

3.5 SEALER APPLICATION

A. Allow a minimum of 48 hours drying time prior to application of protective finish, or as recommended by manufacturer.

B. Apply Meoded Stain Shield sealer in accordance with manufacturer’s written instructions.

C. Remove excess material and ensure uniform appearance. Final appearance may vary depending on application technique and field conditions.

D. Application of protective finish is required to enhance durability and resistance to environmental exposure.

E. Sealer selection and application shall be appropriate for exterior exposure conditions.

3.6 CLEANING

A. Remove masking and protection materials.

B. Clean adjacent surfaces without damage.

C. Clean tools immediately after use.

3.7 PROTECTION

A. Protect finished surfaces from damage during construction.

B. Repair damaged areas to match approved finish to the extent achievable based on hand-applied finish characteristics. Exact matching of repaired areas may not be achievable due to inherent variation of the system.

C. Protect completed work from exposure to adverse weather conditions until fully cured.

3.8 AESTHETIC INTENT

A. Final finish shall exhibit natural variation in tone, texture, and movement inherent to hand-applied lime-based finishes.

B. Finished work shall be evaluated based on approved mock-up.

C. Variations in appearance resulting from hand application techniques and individual applicator methods are inherent to the system and shall not be considered a defect, provided such variations are within the general range established by the approved mock-up.

D. Additional variation in color and texture may occur due to exposure to weather, UV radiation, and environmental conditions and shall not be considered a defect.

© Meoded Paints & Decoration, Inc. Document may be copied by design and construction professionals for use in preparing project specifications for Meoded products. Meoded and product names are trademarks of Meoded Paints & Decoration, INC.

Revision Date: April 2026